## Slide 1: Geotechnical Grout selection
Alan A. Campoli, respec
BRAD YODER, Tri-state Water stoppers
Chris Moore, Cowin

## Slide 2: Cement vs chemical Grouts
  Long debated choice
  Chemical used for wider spectrum of problems
  Chemical developed in the 1960’s
  Choice depends on geologic issues
  Chemical yield
    Greater compressive strength
    Increased tensile strength
    Lower viscosity
    Variable set times

## Slide 3: Grout types
Silicate
Acrylate
Polyurethane

## Slide 4: silicates
  Sodium or Urea based
  Consolidation of loose strata
  Pre-excavation grouting
  Temporary shoring
  Consolidation of fine soils and sands
  Can yield 5000 psi compressive

## Slide 5: Sodium Based
  Penetrate small voids
  Ultra low viscosity (4-8 cps)
  200 psi compressive strength in 24 hours
  Consolidate fine soils and sands
  Not effected by water
  Heaver than water
  Will fall to bottom of standing water
  Underpinning
  Tie-back walls
  Soil nailing

## Slide 6: Urea based
  Two-part system
  Foams up to 30 times liquid volume
  Foam 4 lb/square foot density
  Low exothermic reaction
  Stops water ingress or egress
  Ultra-low viscosity (4-8 cps)
  Cures in 24 hours
  Tunneling face or canopy support
  Low cost as compared to other chemical grouts
  High volume pumping

## Slide 7: Acrylates
  Two-part system
  Low viscosity (4-8 cps)
  Safe and workable
  Hardener is water with metal salt
  Acrylic resin mixed with promoter
  No expansion
  Hard rubber to flexible gel
  Soil consolidation
  Waterproof curtain walls
  Crack sealing
  Simple cleanup

## Slide 8: polyurethanes
  Widely used
  Foam, gel, or high compressive masses
  Hydrophilic formulations
    Single component with catalyst
    Expands 5 to 10 times
    Gel or flexible foam
    Requires water in strata for activation
  Hydrophobic formulations
    Single or two component
    Flexible foam to high strength solid
    Wide range of viscosities
    Tiny cracks to wide voids
    Wide range of expansion and gel times
    Requires void space

## Slide 9: Case study
  Multi level marble mine
  700 ft deep
  Karstic fracture system between mine and reserves
  Two entry access required
  High pressure water connected to surface
  Previous crossing with cement grouting unsuccessful
  Geologic assessment of fracture system
  Polyurethane grouting in advance of mining

## Slide 10: Geologic assessment
  Core drilling on three levels
  Model fracture system on 700 ft level
  Ground water monitoring
  Fractures connected to surface
  Water pressure over 200 psi at 700 level
  Water flows vertically and horizontally in fractures
  Fractures as wide as 15 feet
  Predicted fractures limited to 5 feet in 700 level
  Wider fractures could not be ruled out

## Slide 15: Planned Mining procedure
  Drift advancement in 15 ft rounds
  Simultaneous advancement of A and B
  A kept 50 ft in advance of B
    Guard against simultaneous fracture exposure
    Lateral grout flow to minimize grouting in B
  30 ft exploratory holes before each round
  Water flow immediately stopped with mechanical packers
  Drilling through packers to 30 ft depth
  Grout to stop water flow
  12,000 gallons of three formulations estimated
  16,000 gallons to complete the project
  Current TTL price $45 a gallon

## Slide 26: Grouts employed
Tsw/jsc flex
  Single component flexible hydrophobic grout
  Reaction time controlled by catalyst
  Slow set allowed long distance pumping
  Filled the exploratory boreholes to fracture zone
  Foamed as expected
  Compressed into impermeable plug when hole filled

## Slide 27: Grouts employed
TSW INSTA-SET
  Two component hydrophobic resin
  2.5 pounds per cubic foot density
  High yield expanding 24-30 times
  Compressive strength of 25 psi
  Set time fast to penetrate 30 ft injection
  Use discontinued early in project

## Slide 28: Grouts employed
TSW AG-4
  Two component hydrophobic resin
  4 pounds per cubic foot density
  Medium yield expanding 18 times
  Compressive strength of 80 to 100 psi
  Used exclusively after TSW INSTA-SET discontinued
  Filled fractures along 30 ft injection holes
  Immediately moving water across the face
  Migrated 25 ft laterally in wide fractures

## Slide 30: Project modification
  Entry A encountered a +5 ft lateral void
  Entry A abandoned
  Entry B completed
  Entry C mined on opposite side of entry A
  Grout pumped in entry B visible in entry C

## Slide 33: Conclusion
Stable mine layouts can be designed with good understanding of rock being mined
Problem areas can be identified by geologic mapping.
Numerous grouting options are available.
Support methodology must be compatible with geologic conditions.